Product Name:  ZT4024

Appearance:   A mauve color, free flowing powderwith a bland metal luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                     45-55             12001-26-2             77019

Iron(III) Oxide(Fe2O3)           45-55             1309-37-1              77891

Particle Size Distribution: 80% within the range5-25µm.        (By Malvern Mastersizer2000)

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-8.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     40-70 g oil/100g powder         GB 5211.15-88

Bulk Density:                       10-40 g/100cm3               GB/T 23771-2009

Density                            3.0-3.6 g / cm3 (water=1)