Product Name:  Gold Luster SeriesZT5302

Appearance:   A free flowing off gold powder with a bland luster.

Ingredients and Composition

Chemical Name               %               CAS No.          CI No.

Mica                    50-60             12001-26-2           77019

Titanium Oxide(TiO2)             20-25             13463-67-7           77891

Iron(III) Oxide(Fe2O3)            20-25              1309-37-1           77491

D50

Particle Size Distribution: 80% within (10-40) µm         (By Malvern Mastersizer3000)

18.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0 -11.0                   GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     60-90g oil/100g powder         GB 5211.15

Bulk Density:                       15-30 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)