Product Name:  Gold Luster Series ZT5301

Appearance:   A free flowing off gold powder with a bland luster.

Ingredients and Composition

Chemical Name               %               CAS No.          CI No.

Mica                    48-56             12001-26-2           77019

Titanium Oxide(TiO2)             22-26             13463-67-7           77891

Iron(III) Oxide(Fe2O3)            22-26              1309-37-1           77491

D50

Particle Size Distribution: 80% within the range 5-25 µm       (By Malvern Mastersizer2000)

11.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0 -11.0                   ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90g oil/100g powder        GB 5211.15-88

Bulk Density:                       15-30 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)