Product Name:  5Y25A

Appearance:    A free flowing off white powder with a fine gold reflection color.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                    43-48              12001-26-2             77019

Titanium Oxide(TiO2)           52-57               13463-67-7             77891

Tin Oxide (SnO2)                 1-2                18282-10-5             77861

D50

Particle Size Distribution: 80% within the range5-25µm.        (By Malvern Mastersizer2000)

12.5±1.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           7.0-10.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-80 g oil/100g powder         GB 5211.15-88

Bulk Density:                       20-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)