Product Name:  Exterior Flash Penguin White 96151WR

Appearance:  A white color, free flowing powder with a flash luster

Ingredients and Composition

Chemical Name              %                CAS No.              CI No.

Synthetic mica                80-85              12003-38-2

Titanium Oxide(TiO2)            12-16              13463-67-7               77891

Tin Oxide (SnO2)                  <1                18282-10-5               77861

Cerium Oxide (Ce2O3)               <1                1345-13-7                77280

Polymer                   1-5

D50

Particle Size Distribution: 90% within (25-100)µm.         (By Malvern Mastersizer3000)

47.5±2.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     70-90 g oil/100g powder        GB 5211.15

Bulk Density:                       25-45 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)