Product Name:  Exterior Penguin White 96173WR

Appearance:  A white color, free flowing powder with a bland luster.

Ingredients and Composition

Chemical Name              %               CAS No.               CI No.

Synthetic Fluorphlogopite          63-65             12003-38-2

Titanium Oxide(TiO2)            30-32             13463-67-7               77891

Tin Oxide (SnO2)                  <1              18282-10-5               77861

Cerium Oxide (Ce2O3)                <1              1345-13-7                77280

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range10-45µm.         (By Malvern Mastersizer2000)

20.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       20-45 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)