Product Name:  Exterior Sunny Gold 9305WR

Appearance:  A free flowing off gold powder with a bright luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                   44-48              12001-26-2             77019

Titanium Oxide (TiO2)            28-31              13463-67-7             77891

Iron(III) Oxide (Fe2O3)            17-20              1309-37-1              77491

Tin Oxide (SnO2)                  <1               18282-10-5             77861

Cerium Oxide (Ce2O3)                <1               1345-13-7              77280

Polymer                   1-5

D50

Particle Size Distribution: 90% within（10-60）µm.         (By Malvern Mastersizer3000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15

Bulk Density:                       40-60 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)