Cosray Colored Coloron(Code:89HR2)

INCI Name:    Calcium Aluminum Borosilicate,Titanium Dioxide, Tin Oxide, Red 27 ,Silica

Chemical Composition:                                                                                                       Test method

Calcium Aluminum Borosilicate         50.0-60.0%                                                         CLRTM -51

TiO2                                                          5.0-15.0%                                                            CLRTM -48

SnO2                                                           ≤2.0%                                                              CLRTM -48

SiO2                                                                                           25.0-35.0%                                                       CLRTM -48

FD＆C  Red 27 Al Lake                           10.0-15.0%                                                          CLRTM -48

Appearance:                                          Golden Red-Rose Red                                           CLRTM -52

Odor:                                                        Odorless                                                              CLRTM-53

Particle Size:                                          10-125μm                                                               CLRTM -42

pH-Value(10% Aqueous Suspension): 4.0-9.0                                                                  CLRTM -45

Oil Absorption:                                      30-70g/100g                                                          CLRTM -46

Density                                                    2.4-2.9g/cm3                                                          CLRTM -47

Microbiology:                                         <100 cfu/g                                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                      CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Ba                                                             <50ppm

Cd                                                             <5ppm

Cr                                                              <100ppm

Cu                                                             <50ppm

Ni                                                              <200ppm

Zn                                                             <100ppm