Product Name:  Merck gold  SW6305M

Appearance:  Golden powder.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                    28-41              12001-26-2             77019

Titanium Oxide (TiO2)             55-61              13463-67-7             77891

Tin Oxide (SnO2)                  ≤1               18282-10-5              77861

Diiron trioxide（Fe2O3）            4-10              1309-37-1              77491

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range10-60µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           6.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     55-75 g oil/100g powder        GB 5211.15-88

Bulk Density:                       35-43g/100cm3              GB/T 23771-2009

Density                            3.2-3.6g / cm3 (water=1)