Product Name:  7G218

Appearance:   A free flowing powder with a super bright green luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Fluorphlogopite           28-32             12003-38-2

Titanium Oxide(TiO2)            66-70             13463-67-7              77891

Tin Oxide (SnO2)                  2-4               18282-10-5             77861

D50

Particle Size Distribution: 80% within the range8-35µm.        (By Malvern Mastersizer2000)

18.0±1.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-9.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-80 g oil/100g powder         GB 5211.15-88

Bulk Density:                       45-60 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)