| ## Raystar Glitter Green RS8297 |  |  |
| --- | --- | --- |
| ## Assay | ## Spec. Values | ## Test Method |
| ## Calcium Aluminum Borosilicate | ## 76.0-86.0% | ## CRTM-51 |
| ## TiO2 | ## 14.0-24.0% | ## CRTM-48 |
| ## SnO2 | ## ≤0.6% | ## CRTM-48 |
| ## Particle Size | ## 50-300µm | ## CRTM-42 |
| ## PH Value | ## 4-11 | ## CRTM-45 |
| ##### Density: | ## 2.2-3.2g/cm3 | ## CRTM-47 |
| ## Oil absorption | 50-110g/100g | ## CRTM-46 |
| ## Aluminum Silicate CAS No: 1344-09-8; TiO2:C.I.No:77891; |  |  |