Product Name:  RS8167

Appearance:  A free flowing off white powder with excellent effect of very flash diamond white.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Calcium Aluminum Borosilicate      96-99              65997-17-3

Titanium Oxide (TiO2)             1-4               13463-67-7             77891

Tin Oxide (SnO2)                   <1              18282-10-5             77861

D50

Particle Size Distribution: 90% within the range50-350µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5% max.                 GB 5211.3-85

Oil Absorption:                     50-80 g oil/100g powder        GB 5211.15-88

Bulk Density:                       30-60 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)