Product Name:  Diamond Series KC9810X

Appearance:  A free flowing off white powder with excellent effect of fine diamond white.

Ingredients and Composition

Chemical Name                %               CAS No.            CI No.

Calcium Aluminum Borosilicate            90-95             65997-17-3

Titanium Oxide(TiO2)             5-10             13463-67-7             77891

Tin Ooxide (SnO2)                 <1              18282-10-5             77861

D50

Particle Size Distribution: 80% within the range10-40 µm.         (By Malvern Mastersizer2000)

18.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0 -11.0                   ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       30-60 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)