Cosray Golden Red

(Code: 4213RY)

INCI Name:                                                  Mica, Titanium Dioxide, Tin Oxide, Red 40 Lake

Chemical Composition:                                                                                               Test method

Mica                                                                   41.0-60.0%                                          CLRTM-51

TiO2 (Rutile)                                                      35.0-43.0%                                          CLRTM -48

FD&C Red 40 Al Lake                                     5.0-15.0%                                             CLRTM -48

SnO2                                                                      ≤1%                                                CLRTM -48

Appearance:                               Red Powder with Interference Gold                         CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             45.0-95.0g/100g                                      CLRTM -46

Density                                                               2.3-3.2g/cm3                                              CLRTM -47

Microbiology:                                                 <100 cfu/g                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <20ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm