Cosray Crystal Glitter Yellow Gold

(Code: 6371C)

INCI Name:      Synthetic fluorphlogopite, Titanium Dioxide, Iron Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                70.0-90.0%                                             CLRTM-51

TiO2                                                                 8.0-20.0%                                               CLRTM -48

Fe2O3                                                            5.0-15.0%                                                CLRTM -48

Appearance:                                               Glitter Yellow Gold                                    CLRTM 52

Odor:                                                                Odorless                                                CLRTM -52

Particle Size:                                                   40-200μm                                               CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                          50.0-90.0g/100g                                         CLRTM -46

Density                                                             2.5-3.2g/cm3                                                CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Sb                                                              <2ppm

Ba                                                             <50ppm

Cd                                                             <1ppm

Cr                                                              <100ppm

Cu                                                             <50ppm

Ni                                                              <200ppm

Zn                                                             <50ppm