Cosray Crystal Ultra Sparkle Green

(Code: 6275C)

INCI Name:                                          Synthetic fluorphlogopite, Titanium Dioxide，Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                70.0-82.0%                                             CLRTM-51

TiO2 (Rutile)                                                    18.0-30.0%                                             CLRTM -48

SnO2                                                                  ≤1.0%                                                CLRTM -48

Appearance:                                               Glitter Interference Green                       CLRTM 52

Odor:                                                                Odorless                                                CLRTM -52

Particle Size:                                                   40-200μm                                               CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                          50.0-90.0g/100g                                          CLRTM -46

Density                                                             2.5-3.5g/cm3                                                CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm