Cosray Rrystal Sparkle Red

(Code: 6252C)

INCI Name:                                         Synthetic fluorphlogopite, Titanium Dioxide, Tin Oxide

Chemical Composition:                                                                                               Test method

Synthetic Mica                                         72.0-84.0%                                                   CLRTM-51

TiO2                                                          16.0-28.0%                                                   CLRTM -48

SnO2                                                              ≤1.0%                                                     CLRTM -48

Appearance:                                             Sparkle Red                                                  CLRTM 52

Odor:                                                            Odorless                                                    CLRTM -52

Particle Size:                                                10-125μm                                                  CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                         45-95 g/100g                                                CLRTM -46

Density                                                           2.5-3.5g/cm3                                                   CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm