Product Name:  Multi-Colour Series 2512S

Appearance: A free flowing off white powder with a green/gold/white/red multicolor effect.

Ingredients and Composition

Chemical Name               %               CAS No.             CI No.

Synthetic Fluorphlogopite            30-40             12003-38-2

Titanium Oxide(TiO2)             16-22             13463-67-7              77891

Tin Oxide (SnO2)                  <2               18282-10-5              77861

Cobalt(III) Oxide(Co2O3)          2-4              1308-04-9

Silicon Oxide (SiO2)            38-48               7631-86-9

D50

Particle Size Distribution: 80% within ( 10-45)µm.        (By Malvern Mastersizer3000)

25.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           5.0 -8.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15

Bulk Density:                       30-60 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)