Cosray Crystal Ruby

(Code: 6428RC)

INCI Name:                       Synthetic fluorphlogopite, Titanium Dioxide, Carmine, Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                  69.0-84.0%                                           CLRTM-51

TiO2 (Rutile)                                                      14.0-22.0%                                           CLRTM -48

Carmine                                                             2.0-8.0%                                              CLRTM -48

SnO2                                                                     ≤1.0%                                              CLRTM -48

Appearance:                                                 Red Pink Powder                                    CLRTM -52

Odor:                                                                   Odorless                                             CLRTM -53

Particle Size:                                                    10-125μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                  CLRTM-45

Oil Absorption:                                             50.0-90.0g/100g                                       CLRTM -46

Density                                                               2.5-3.5g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm